IRON & STEEL

A while ago I wrote a feature about carbon-fibre, because it's an

up-to-the-minute trendy sort of material. Even its name sounds so

ace,  race, on the pace. In reality, I should have  started  with

steel  because  it's better and stronger and more useful  in  any

number of ways.

Steel is very strong. People are used to  hearing

this,  and they tend to miss just how strong it is.  Forget  your

titanium, your CFRP (carbon-fibre reinforced polymer  composite),

size-for-size steel is stronger than all of them - and by quite a

long shot. It can be made pretty tough, too.

It's  no use me trying to impress you with figures  like  270,000

psi  UTS  or 2,000 MN/sq.m. Like most people, I find  numbers  by

themselves  utterly  meaningless, so let me help you try  to  get

your  heads  around  just what sort of strength  we  are  talking

about. Suppose you were going to fix a box to the ceiling using a

single bolt, of really high-spec steel, one inch in diameter.

What do you think you could put in the box? A man? Yes, surely  -

even  a  20-stone man (to our readers in the US, 20st  is  280lbs). Maybe two men,  even. After all, a one-inch diameter steel bolt is  a pretty chunky size. So do you reckon you could put something else even  heavier  in the box, like a Honda Fireblade  (which  weighs about 30 stones)?

Well,  I've  pushed  this one far enough. In  truth,  using  that

single  steel bolt, you could hold up 300 (three hundred,  that's

not a typing error) Blades, EACH ONE WITH A 20st RIDER SITTING ON

IT.  Three  hundred FireBlades and three hundred  FatBlokes,  all

hanging  off a single one-inch steel bolt. Think about it  for  a

while.

Right, now some history. The progress (if you could call it that)

of  the  earth's peoples has been driven through the ages  by  an

overwhelming  desire  for  them  to kill  each  other  ever  more

efficiently.  Rocks  and clubs gave way to  flint-tipped  spears,

copper  and bronze arrow-heads, iron axes, steel swords and  gun-

barrels, jet fighters, chemical warheads,  nuclear missiles,  etc

etc.  Iron was a natural progression; it made better  swords  and

cannons than bronze.

Rather than just giving you this as a glib statement, let me show

you  an example. People often have a go at me about  the  obscure

sources  I use to back my theories, so here's another one  you'll

like. It was quite a best-seller of a desert skirmish, a sort  of

prequel  to  Bravo Two Zero. Everyone knows the story  about  the

most famous fight between a Biblical Israelite and a Philistine:

"So David prevailed over Goliath with a sling and with a  stone,

and smote the Philistine and slew him."

(First Book of Samuel, chapter 17, verse 50).

The point here is that David had no choice but to use his  sling,

because  if  he had let Goliath anywhere near him it  would  have

been  all  over in seconds - the Philistines had learned  how  to

make  iron swords, daggers and spear-points; they even  had  iron

tyres   to  keep  their  wooden  chariot  wheels  together.   The

Israelites were still using bronze swords and copper shields, and

wouldn't  have  stood a chance in close-quarter fighting.  So  if

David  hadn't  scared  off  the  Philistines  before  the  battle

started, the Israelites would have been wiped out, there would be

no  Jews  and no Christians, and we wouldn't now have  the  quote

from George Gershwin's Porgy & Bess (1935):

Things that you're liable

To read in the Bible

Ain't necessarily so.

The best guess we can make about how iron was first discovered is

the  theory that it was smelted by accident when someone  made  a

campfire on ground which was rich with iron ore; or maybe someone

used a type of iron ore (haematite) for colouring pottery in  his

kiln and found it like that.

Either  way,  small  spongy  lumps of  low-grade  iron  would  be

produced,  which would have attracted attention because  even  in

that  poor state, full of impurities, they would have  been  hard

enough  to  scratch a bronze sword. The spongy lumps  would  have

been  hammered into useful shapes after reheating,  so  producing

what we now call wrought iron. We don't know too much about early

iron  weapons, simply because archaeologists don't dig them up  -

if  the  exhaust  of a GPz550 can rust away to  nothing  in  five

years, what chance is there of finding a seven thousand year  old

sword blade?

I'll  now  neatly  skip  a few thousand  years  of  history,  and

describe modern iron smelting using a blast furnace (by  "modern"

I  mean that they haven't changed all that much in the  last  200

years).

The best iron ore contains about 60 to 65% iron, but we have  now

used  most  of the good stuff, and we have to mine  poorer  grade

ore. This is crushed into rubble, and loaded into the top of  the

furnace  together  with coke and limestone. The  single  greatest

advance in iron smelting was the invention of the "blast," a  jet

of  superheated  air  which  is forced into  the  bottom  of  the

furnace, and this increases the burning efficiency enormously.

A  blast furnace is about 100 feet high, and  works  continuously

for  months at a time. You just keep loading ingredients  in  the

top, and using the gas which is given off to heat the air for the

blast at the bottom. The temperature at the bottom of the furnace

is  about 2,000 centigrade, and molten pig-iron can be drawn  off

through  a  hole. Most of the impurities from the  ore,  together

with what's left of the coke, combine with the limestone to  form

a  waste residue called slag which floats on top of the iron  and

can also be poured off through another hole. This waste tends  to

get used as an aggregate for the building materials industry.

The  pig-iron  coming  out of a blast surface is  useless  as  an

engineering  material. It contains 3 to 5% carbon from the  coke,

and lots of silicon, manganese, phosphorus, and sulphur -  making

it  brittle.  Years  ago, pig iron wold have  been  remelted  and

refined  by labour-intensive forging to make into  wrought  iron,

but  now  it  tends to go directly for  steelmaking.  Cast  iron,

incidentally,  is hardly ever made from pig-iron these days;  the

economics of the process mean that it is generally produced  from

reclaimed scrap iron and steel - i.e. steel from which the excess

carbon has been refined has it added back again, to make it  into

lower-grade stuff for resale. If you understand the economics  of

this process, please write to me and explain them.

We  tend not to see too much grey cast iron on bikes these  days,

but   spheroidal  graphite  iron  brake  discs  are   common, and calipers are also sometimes still made out of  it.

I  saw  a gearbox selector drum made out of cast  iron  recently,

which  I thought was a good idea, but they're usually  steel.  We

also see this type of iron used for camshafts and the chainwheels

on  them. An excellent use for cast iron is turbo  housings,  but

there aren't too many of those on bikes.

"Cast  iron"  is used to describe iron in which more than  2%  of

carbon  is dissolved. Anything with less than 2% is  steel.  Cast

iron  isn't  as strong as steel, neither is it anywhere  near  as

tough or as ductile. The beauty of the stuff is in its ability to

be  cast into all sorts of complex shapes very easily  -  cutting

down on the forging or machining operations needed if you  wanted

to  make the same bit out of steel.

When  you  do come to machine cast iron, you find  that  all  the

dissolved  carbon in it acts like a solid lubricant, so  you  can

get a really nice finish easily and quickly. Because of this, you

don't  have to run coolant over the job as you're  machining  it,

which  is  rather pleasant as your trousers don't  get  wet.  The

flip-side  is that the fine powdery carbon in the  cuttings  gets

everywhere and your snot goes black for days afterwards.

In case you're thinking of cast iron as a rather cheap and  crude

structural  material, consider that in the days  of  turbocharged

formula  1  cars, when 1500cc engines were  producing  well  over

1,000bhp  in  qualifying  trim (and not much  less  over  a  race

distance) the most successful engines - Honda, Renault, and BMW -

were using iron blocks most or all of the time. Certainly,  Honda

never  used  anything  else,  and as they  were  rumoured  to  be

spending  $140m a year on F1 engines, economics can't  have  been

too far up their list of priorities when they were deciding  what

to make the block out of.

Steel is much more interesting to us bike enthusiasts, in fact it

is a fascinating subject for all engineers. All steels are alloys

of  iron  and  carbon,  and some  have  small  amounts  of  other

additives  like silicon, copper, manganese,  phosphorus,  nickel,

chromium,  molybdenum (everybody's heard of  chrome-moly  tubing)

etc.  The range of properties available to us simply  by  varying

the composition, the refining process, and the heat-treatment  is

mind-boggling.  It's  the difference between a crankshaft  and  a

valve-spring,  an exhaust pipe and a big-end bolt. We  are  still

learning more and more about steel.

There are reasons why the properties can be varied so much  which

are very simple in principle and horrendously complex in  detail.

Very clever metallurgists spend their whole working lives  trying

to  get  to  grips with the details, often  without  making  much

progress.    The    basics   revolve    around    polycrystalline

microstructures,  which is what any steel is, and it's easier  to

understand  how they're formed by thinking about  something  more

familiar to us, like salt.

You  can dissolve salt in a glass of water, but only so  much  of

it.  You get to a point when no more salt will dissolve, and  any

extra you put in just stays as grains in the bottom of the glass.

The water-salt solution is then said to be "saturated."  However,

if  you  heat  the water, more salt will dissolve,  and  you  can

probably  get all of the salt grains to disappear.

The same thing happens with water and air. Saturated air is  100%

humidity;  75% humidity just means that the air  contains  three-

quarters  as  much  water  as would saturated  air  at  the  same

temperature  and  pressure. If you reduce the  pressure  (say  by

blowing  the air over a mountain) or you reduce  the  temperature

(by passing the air over a lake) water will often precipitate out

as small droplets (mist) or big ones (rain).

Back to our salt in the glass. If you allow the mixture to  cool,

some of the salt will then start to fall out of the solution  and

reappear   as  a  solid  -  the  scientific  term  for  this   is

precipitation.  If  you're  very careful, and you  can  cool  the

mixture  slowly  and  evenly, you can grow  a  single  huge  salt

crystal like this (in fact, the best way of doing it is to  start

off  with a cold solution of water and salt, and then reduce  the

amount of water mega-slowly by letting it evaporate over a period

of several days).

Growing  big  salt  crystals like this is  a  standard  chemistry

experiment  for  schoolkids.  What usually  happens  outside  the

chemistry lab is that the water cools so quickly that instead  of

getting  one  big grain of salt, you end up with lots  of  little

ones  because  molecules of salt precipitate out  on  their  own,

instead  of growing on to each other. This basis is  exactly  the

same  set-up as you have with molten iron which has  some  carbon

dissolved in it.

When  iron has only a little carbon dissolved in it,  the  carbon

atoms distort the matrix of the iron atoms. This is a good thing,

generally  -  the  distortion means that the iron  atoms  in  the

matrix  can't  slip  around over each other  so  easily,  so  the

material  becomes more difficult to deform. Now, if you cool  the

iron mix slowly, you tend to get big grains of iron, so the whole

thing  appears quite ductile, but not too hard. Cool it  quickly,

and  you  have  the opposite effect - lots of  small  grains  are

generally  hard, but brittle. Of course, if the amount of  carbon

in  the iron is anywhere near saturation point, you end  up  with

grains of iron-carbon alloy, and also grains of pure carbon which

have precipitated out during the cooling process.

This, again, can be a good thing. Bits of solid alloying  element

(called  inclusions) can act as little pegs to stitch  individual

grains  of iron together. You can have too much of a good  thing,

though  - if there are too many inclusions, or they are too  big,

they  will weaken the structure. Modern  steel-producing  methods

usually  keep  a tight control of inclusion size, but  in  really

critical situations it's a good idea to examine bits by x-ray  to

check for voids or excessively large inclusions.

I  once examined the remains of a formula 1 racing  engine  which

had put a rod through the side of the block during a GP; the  rod

had  snapped  clean in two and the failure started  at  a  carbon

inclusion  so big that it looked like a lump of coal,  about  1mm

across. I kept the rod on my desk as a paperweight and showed  it

to people for months, and just before Christmas the man from  the

steel  company asked me if he could have it as a gift. I  agreed,

so he picked it up, walked outside, and threw it in the river.

When  the  only  alloying element in the steel  is  carbon,  it's

generally  known  (obviously enough) as carbon  steel;  or,  more

particularly, low-carbon, medium-carbon, or high-carbon. In  each

case, the difference is only a fraction of a percent. Adding more

carbon  tends  to make the steel stronger and  harder,  but  more

brittle and less ductile.

There   are  other  favourite  ingredients   that   metallurgists

routinely  throw  into  the mix, and I'll go  through  the  usual

suspects. Chromium is excellent stuff, it increases the strength,

hardness,  toughness, wear-resistance, and  corrosion-resistance.

It  can  also be a bitch to machine. Steels with  more  than  10%

chromium  in  are  known  generically  as  stainless,  and  these

normally  have a lot of nickel in, too.  Nickel is also good  for

hardness  and toughness, and is useful because it doesn't have  a

bad  effect  on the ductility like carbon  does.

Cobalt  increases hardness and toughness, and is often  found  in

steel  used  for  cutting tools.  Sulphur makes  the  steel  much

easier  to  machine,  but  doesn't  do  anything  for  the  other

properties  and makes welding a nightmare. On the other  hand,  a

certain amount of silicon makes welding much easier.

Some  alloying  elements  are  used  because  they  improve   the

properties  of the steel at high temperatures, like tungsten  and

molybdenum. Others, like vanadium, cobalt, and manganese, tend to

make the steel respond better to processes like heat treatment  -

of which more later.

The mix of dissolved carbon and free carbon, dissolved alloy  and

free alloy, and the size (and shape) of the grains thereof,  give

an  endless number of ways of varying the properties and  totally

confusing  yourself.

There are endless stories about types of steel which have  proved

disastrous  in service for some reason that nobody noticed  until

it was too late. A good example was the use of stainless steel in

the  first  replacement hip operations; something in  the  bodily

fluids  attacked  the  steel and turned it  so  brittle  that  it

snapped like a carrot in no time at all. This is why we  now

have  a  special grade of steel called "medical  stainless"  with

which  Mr Sheene, Mr Schwantz, and Mr Doohan are all familiar  to

varying degrees.

There  is  a  theory  kicking around  that  the  reason  why  the

"unsinkable"  Titanic seemed to roll over and die so quickly  was

that the particular type of steel used for its main structure was

fine  when  tested  at room temperature  but,  unusually,  became

horribly weak after it had been in freezing cold sea-water for  a

while.

This  neatly brings me on to heat-treatment of steels.  While  we

can  get  excellent results by taking care over how we  cool  our

steel mixes from the molten state, things can also be tweaked  on

some  types  of  solid steel by heat-soaking them  at  a  certain

temperature and then cooling them at a carefully controlled rate.

Most metals (but not aluminium) have a critical temperature.  For

steel,  it's  about  850  centigrade,  above  which  the  crystal

structure  changes from the 9-atom body centred cell to  the  12-

atom  face centred cell. By heating it to above this  temperature

(which is well below the melting point, 1500 centigrade) and then

being  careful about how rapidly we cool it, we can control  what

sort  of crystal structure we end up with, and how  the  alloying

elements are combined with it.

The  general  effects  of  heat treatment  are  to  increase  the

hardness  (but  also  the brittleness)  by  cooling  rapidly,  or

achieving  the  opposite  effect by  cooling  it  slowly  (called

annealing).  This  can be done before or  after  machining;  it's

obviously very convenient to machine something when it's as  soft

as shite, then turn it glass-hard afterwards, but in practice  the

component will often distort too much.

By tweaking the production methods, we can come up with  material

that is stiffer than carbon-fibre, stronger than carbon-fibre, as

tough  as  anything  you can think of,  harder  than  glass,  and

varying  in price from less than wood to more than gold.  There's

nothing an engineer can't make with steel - if you don't  believe

me, ask a rugby player to sing you the song.